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	Technical Data 


	Film thickness:
	
	approx. 120 µm

	Composition:
	
	100% PVC, monomeric

	Basic weight:
	
	approx. 115 g/m²

	Surface:
	
	Sand effect structure

	Adhesive:
	
	Highly transparent, solvent-based acrylic adhesive, permanent

	Adhesive thickness:
	
	25 g/m²

	Adhesive strength on glass:
	
	24h > 18N/25 mm

	Liner:
	
	65 g/m² Glassine paper, single side siliconized

	
	
	

	
	
	

	General Information


	•
	100% polyvinyl chloride, monomeric plasticised

	•
	Single-sided self-adhesive, scratch-resistant, finely embossed transparent PVC film

	•
	Washable and resistant to various cleaning agents and solvents

	•
	Made with a solvent-based, ageing resistant and permanently elastic acrylate adhesive

	•
	B1 Flame retardant certified according to the DIN 4102 norm

	•
	Floor slip resistance according to class R9 according to DIN51130

	
	

	
	

	
	

	Application



	•
	Protective and finishing film for classic photos and digital prints

	•
	Universal uses for indoors so as short to medium term outdoors applications

	•
	Due to the scratch-resistant surface, it is ideal for mechanical laminations, such as the creation of display panels 
for pop-ups

	
	

	Advantages



	•
	Improved quality, almost no silvering ghost effects after lamination

	•
	Very good behaviour of the adhesive

	•
	Scratch-resistant surface

	•
	Suitable for many materials printed with UV inks

	
	

	
	

	
	

	
	

	
	

	
	

	
	

	Processing instructions


	•
	When laminating on inkjet prints, it must be fully dried. A drying time of 24 hours is recommended

	•
	The optimum working conditions during processing is between 18° - 25°C and a relative humidity of 40% - 65%

	•
	We recommend using cold lamination for this product.

	
	

	
	

	More information 



	•
	You can find more information on our products on www.com2-c.de

	•
	Always store rolls together with the label or batch number. No complaints can be processed without a 
batch number.

	•
	Shelf-life of this product is approx.12 months.

	•
	Our tests are carried in standard climate conditions

	
	

	Available sizes



	•
	50m x 137,0cm (54'')

	
	

	
	This technical information was made and assessed based on the latest technology and our experience. Due to various parameters and conditions under which the described product is used, we re-commend that every user should check the product for its suitability for the intended uses. A legally binding assurance of certain properties cannot be derived from our information. Errors and changes are subjected. With the release of a new version, this datasheet version will not be valid.
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