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	Technical Data



	PP Film thickness:
	
	100 µm

	Total thickness:
	
	approx. 280 µm (incl. adhesive and liner)

	Composition:
	
	PP (BOPP) + transparent reversible acrylic adhesive + embossed paper, single sided siliconized, double-sided PE coated

	Liner:
	
	140 g/m² embossed, double-sided PE-coated paper

	Surface:
	
	matte white

	Adhesive:
	
	Transparent, Water-based, Removable acrylic adhesive

	Flame Retardancy:
	
	EN 13501-1:2019 

	

	General Information



	•
	100 µm white matte biaxial oriented (BOPP) polypropylene film

	•
	100% PVC free

	•
	Flame retardant according to European standard EN 13501-1:2019

	•
	Recyclable

	•
	No VOC emissions (volatile organic compounds)

	•
	Bubble-free adhesion

	•
	Reversible/removable adhesive

	•
	Suitable for indoor and outdoor application

	•
	Printable with latex, UV-curable, eco solvent and solvent inks

	•
	Fast drying

	•
	High colour brilliance

	•
	Good water and scratch resistance

	
	

	Application



	•
	Labels, stickers, signs, markings

	•
	Quick and easy interior decoration

	•
	Wall covering

	•
	Events, trade fair and shop fitting

	•
	Short - medium term outdoor application / Signage

	
	

	Advantages



	•
	Environmentally friendly

	•
	Recyclable

	•
	100% PVC free

	•
	Easy, bubble-free application

	•
	Reversible adhesive with good, reliable adhesion

	
	

	
	

	Printing Properties



	•
	Excellent printability with latex, UV curing, eco solvent and solvent inks

	•
	No bleedings even with high ink limit

	•
	Fast drying

	•
	High colour brilliance

	
	

	
	

	Processing instructions



	•
	The print must be completely dry before further processing; a drying time of 24 hours is recommended

	•
	The surface must be dry, clean, absorbent and smooth

	•
	Roller or felt squeegee recommended to be without sharp edges

	•
	To avoid fingerprints, the use of cotton gloves is recommended

	•
	The optimal working condition during processing is 18° - 25°C and a relative humidity of 40% - 65%

	•
	When removing/disassembling, make sure that the GreenFilm is not torn off suddenly, but is pulled off slowly.

	
	

	
	

	More information



	•
	You can find more information on our products on www.com2-c.de

	•
	The print side of the materials as well as the lengths and widths can be customized to your needs prior to a MOQ

	•
	Always store rolls together with the label or batch number. No complaints can be processed without a 
batch number.

	•
	Our tests are carried in standard climate conditions

	•
	Shelf life in the original packaging, 2 years when storing properly at 15° - 20°C

	•
	Durability:  up to 2 years (unprinted, indoor application)

	
	

	
	

	Available sizes



	•
	50 m x 137,0 cm (54´´) 

	
	

	
	This technical information was made and assessed based on the latest technology and our experience. Due to various parameters and conditions under which the described product is used, we re-commend that every user should check the product for its suitability for the intended uses. A legally binding assurance of certain properties cannot be derived from our information. Errors and changes are subjected. With the release of a new version, this datasheet version will not be valid.
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